## Slide 1
Lecture 11: Electrodynamics, non-equilibrium superconductivity, and beyond BCS
Lecture 10: BCS theory --- Temperature dependence, thermodynamics, and coherence factors
Next time
Today
Discussion the BCS theory in four parts:
Clues to the mechanism and the Cooper instability problem
Attractive interaction and the BCS wavefunction and ground state
Self-consistent solution and quasiparticles
Temperature dependence, thermodynamics, and coherence factors
Electrodynamics, non-equilibrium superconductivity, and beyond BCS

## Slide 2
Introduced the Bogoliubov quasiparticle operators:
Leading to:
Last time
Diagonalized the “model” BCS Hamiltonian:
creates a state with occupied and
empty --- all other states are unchanged from the ground state
creates a state with occupied and
empty --- all other states are unchanged from the ground state
ground state
excitations

## Slide 3
Occupation in ground state
Pairing interaction
Effective charge

## Slide 4
Excitation picture
GROUND
STATE
Normal metal
Superconductor
(T=0)
1
1
EXCITATIONS
“electron”
“hole”
holes
electrons
holes
(T=0)
electrons
spin
created in pairs to conserve charge
electron-like qp’s
hole-like qp’s
Quasiparticles do not need to be created in pairs because the ground state charge can change
Also

## Slide 5
OCCUPATION PROBABLILITY
Finite temperature --- thermal activation of excitations
Normal metal
Superconductor
OCCUPATION PROBABILITY
Temperature dependence comes from and
Thermally-activated carriers due to energy gap

## Slide 6
Temperature dependence of the energy gap
Using BCS form for the attractive interaction:
Solve to get 

## Slide 7
Convert to integral  compute
numerically
occurs when
1
1
Gap equation:
For weak coupling (

## Slide 8
empty pair state
qp in
full
pair state
no qp in
Comparing the electron distribution is the normal and superconducting state
Normal metal
At
In general:
Superconductor at T=0
Electron-state occupation does not change much --- the key to superconductivity is the pair correlations induced by the attractive interaction

## Slide 9
Thermodynamics
Excitations are fermions :
(pairing)
redistribution of states by
(NORMAL STATE as
variation of gap with
(SC STATE)

## Slide 10
Low : constant so 2nd term
exponential behavior
High : so 1st term = normal state
finite so jump at
Near
)
)

## Slide 11
Coherence Factors
The processes are different from these in normal metals because of:
different density of states
energy gap
Interference terms coherence factors
Consider a perturbation to system:
something - on
NORMAL STATE ’s are qp operators matrix elements
SC STATE
e.g.
’s are qp operators which involve correlations between states modified
Quasiparticles can scatter, be created (pairbreaking), or be destroyed (recombination)

## Slide 12
qp scattering
qp creation
qp recombination
If we write in terms of qp operators , must add before squaring to get matrix elements:
I. Scalar field (EVEN)
depends on only
e.g. electron-phonon interaction, ultrasonic attenuation
II. Vector field (ODD)
depends on ) only
e.g. electromagnetic fields
Two cases:

## Slide 13
Matrix elements :
(not transition probability which also depends on )
SCATTERING
CASE I
CASE II
)2 =
()2 =
CREATION/ANNIHILATION
CASE I
CASE II
=
=
For E,E’~
1
Integrated over 
For E,E’ 
small difference
large difference between cases

## Slide 14
Examples
Type I Ultrasonic attenuation
Type II Nuclear relaxation
diverges
broadening (finite lifetimes qp’s, unparticles
#qp’s
Great success – impossible to explain by two-fluid model or energy gap modelcoherence vital
rate
occupation
probability
Hebel-Slichter peak

## Slide 15
Coherence Factors
Physical picture:
NORMAL
SUPERCONDUCTING
Electron correlations cause interference between qp transition probabilities selection rule for transitions depending on symmetry of perturbation
constructive interference
# qp’s
example:
destructive interference
e.g. Hebel-Slichter peak in NMR
e.g. rapid decay with temperature in ultrasonic attenuation