## Slide 1
Lecture 19: The dc SQUID --- models
Lecture 18: The Josephson effect --- beyond tunnel junctions (SNS, microbridges, SFS, …)
Next time
Today
Discussion of the Josephson effect in five parts:
Theory and phenomena
RSJ model
Magnetic field effects
Fluctuations and quantum tunneling
Beyond tunnel junctions (SNS, microbridges, SFS, …)

## Slide 2
Plan for the rest of the course

## Slide 3
Final project
27 students
6 groups of 4-5
Explore a topic --- make a set of slides
12 minute presentation on May 12 (last day of class)
Topics:
Conventional superconducting qubits vs. topological superconducting qubits
Superconducting qubits vs. ion trap qubits
Superconducting qubits vs. semiconductor qubits
Quantum Supremacy
Superconductors for Quantum Networking
Superconductors for Quantum Sensing
Quantum computing for discovery of new superconductors
Or a topic of your choosing

## Slide 4
Josephson Effects in Weak Links
tunneling derived for SIS tunnel junction 
(qp)
Josephson effect is more universal  QM description in terms of phase-locking of superconductor islands
How to define Josephson effect?
Not supercurrent common in superconductors
Not
Key property: Periodic CPR
for some phase (usually )
Key experiments: CPR measurements (not common/challenging)
AC-induced steps (steps)
SQUID behavior/diffraction pattern behavior
What is different ?
Critical current vs. T  how excitation suppress superconductivity
Critical current vs. B  current-phase relation
(pair)
(Waldram)

## Slide 5
Types of Josephson junctions
S-N-S normal metal
S-I-S insulator
S-F-S ferromagnet
S-Sm-S semiconductor
S-TI-S topological insulator
S-v-S vacuum (STM)
S-g-S graphene
microbridge
“Dayem bridge” (variable thickness microbridge)

## Slide 6
SNS
N
S
S
PROXIMITY EFFECT
order
parameter
effective
pairing interaction
pair correlation function
– OR –
condensate amplitude
S
F(x)
N
I
I
x
Proximity effect  smears out across the interface
clean
dirty
SC
leakage of Cooper pairs out of S into N
leakage of quasiparticles out of N into S
Results in the spatial variation of parameters
 non-local

## Slide 7
0
S
S
N
N
S
S
SIN
SIS
I
Temperature dependence
Spatial dependence
Critical current

## Slide 8
Microscopic picture
S
S
N
Normal conduction by diffusion through linear How is phase coherence mentioned?
S
N
ANDREEV REFLECTION – process for charge transport across interface
e
h
2e
S
N
electron from N incident on the barrier
hole created in N “retroreflected” to conserve energy and momentum
Cooper pair created in S
probability depends on /
electrons above the gap can find states in the superconductor
electrons below have no available states
picture

## Slide 9
e
h
2e
2e
N
S
S
Forward and back scattered electrons and holes are coherent
broad qp states in N
maintain phase coherence across the junction
“bound states carry supercurrent”
SNS Josephson junction

## Slide 10
Andreev reflection – (1964)
developed to explain as a decrease in the thermal conductivity at low T
I
A
B
D
C
momentum
space
position
space
Blonder-Tinkham-Klapwijk (BTK)
extended by
Bound states reflection & phase coherence  interference
(standing waves)
Schroedinger equations for qp’s
Solve Bogoliubov-deGennes equations
For , decouple into:
define normal qp’s (excitations)
Predicts shape of tunneling characteristics as the barrier height changes

## Slide 11
More oscillations --- the deGennes – St. James oscillations
N
S
Like particle in a box, except near so phase winds
K looks like Schroedinger equation

## Slide 12
Ballistic SNS junction
e
h
S N S
N
evanescent tail
bound state energy
phase diff. evanescent path
finite currents do not cancel  net supercurrent
currents cancel

## Slide 13
Superconductor-Graphene-Superconductor Junctions
High transparency states give higher harmonic contributions to the CPR, inducing skewness
Interferometer technique (Urbana)
Asymmetric SQUID technique (Delft)
C. English et al., PRB 94, 115435 (2016)
Nanda et al., arXiv:1612.06895v2
Titov and Beenaker, PRB 94, 041401 (2006)

## Slide 14
Microbridge solve GL equations
S
S
I
current & piling
Crossover from bulk SC behavior to Josephson behavior
long
wide
short
narrow
Modification of CPR :
Superconducting weak links
K. K. Likharev
Rev. Mod. Phys. 51, 101 (1979)

## Slide 15
0
1
2
3
4
V
I
discrete PSC’s – spread out evenly in principle but pinned by defects in real samples
Phase slip centers:
How does a bridge go normal?
Generates local “Phase slip center” --- like 1D vortex
Non-equilibrium region nucleates when Ic exceeded
I
Charge imbalance --- excess of charge in the qp distribution
I
Quantum phase slips? --- still debated whether PSC can be generated by macroscopic quantum tunneling
(Alexey Bezryadin has studied this)

## Slide 16
Point contact Josephson junctions
SIS?
SNS?
microbridge?
Common technique: “break junctions” --- break a wire and them re-contact
Useful to make clean contacts in exotoc materials, e.g. HTSC

## Slide 17
Order parameter oscillations
Proximity decay
Superconductor-Ferromagnet-Superconductor Junctions
SC order parameter decays AND oscillates due to magnetism --- FFLO state
0
p
0

 ~ nd
 ~ (n+½) d
Can move across the 0- transition by changing the barrier thickness or the temperature

## Slide 18: -Josephson junction
0-junction
minimum energy at 0
I
f
-junction
minimum energy at 
I
f
Spontaneously-broken symmetry
Spontaneous circulating current for bL>1 in zero applied magnetic flux
I = Icsin(+) = -Ic sin
E = EJ [1 - cos(+)]
= EJ [1 + cos]
E
f
E
f
negative critical current


-
2
-2
0

## Slide 19
SFS Junctions --- mapping the 0-junction to -junction transition

M
Current-Phase Relation measurement
Current-Voltage measurement
V. Ryazanov et al. (Chernogolovka)
S. Frolov et al. (Urbana)

## Slide 20
Ic2 ≈ +35mA
Ic2
Ic1
Tp
T = 1.81K
T = 2.27K
T = 2.20K
T = 1.97K
T = 2.40K
T = 2.58K
Origin: rapid spatial changes in the critical
current from 0-junction to -junction
SFS Junctions --- looking for higher harmonics
The vanishing of the first-order Josephson effect allows a search for higher harmonics in the CPR
M. Stoutimore et al. (Urbana)

## Slide 21
Current-phase relation
Order parameter symmetry
Critical current variation
Magnetic field variations
Josephson Interferometry: what it tells you
Gap anisotropy
Domains
Charge traps
Flux focusing
Trapped vortices
Magnetic particles
Unconventional superconductivity
Non-sinusoidal terms
-junctions
Exotic excitations e.g. Majorana fermions

## Slide 22
Effect of non-sinusoidal CPR on diffraction patterns
sin() + sin(2)
sin() + sin(3)
sin() + sin(2) + sin(3)
Skewed CPR
x10

## Slide 23
Experiment
Simulation
SFS: Josephson interferometry measurements
Simulation:
Nb-CuNi-Nb junctions
Observe signatures of the non-sinusoidal CPR in the Josephson interferometry measurements

## Slide 24
Direct measurement of the Current-Phase Relation
Screening technique (Jackel)
Interferometer technique (Waldram)
Junction embedded in SC loop (rf-SQUID)
Inject flux  induces circulating current
Detect flux with SQUID
Junction in SC loop (rf-SQUID)
Inject current  divides according to phase
Detect flux with SQUID
Extract CPR
Ic
Ic
First used to study the properties of superconducting microbridges  skewed CPR arising from an online inductance that gives extra phase

## Slide 25
Direct measurement of the Current-Phase Relation
Dispersive technique (Silver, Deaver, Il’ichev)
Asymmetric dc SQUID technique
Junction embedded in SC loop (rf-SQUID)
inductively-coupled to a tank circuit
Excite with rf signal  induces rf currents
Readout phase shift between Vin and Vout
Extract CPR
Ic1
Ic2
Ic1 << Ic2
Junction embedded in dc SQUID
Apply flux  induces circulating current
Measure critical current vs. flux
Modulation is dominated by the phase evolution of the small junction