## Slide 1
Lecture 2: Defining properties of superconductors
Explore the properties that define the superconducting state:
Zero resistance
Limits to superconductivity: critical temperature, critical magnetic field, critical current
Perfect diamagnetism --- the Meissner effect
Limits to the Meissner effect:
(a) penetration depth
(b) vortices --- Type II superconductivity
(c) anisotropy --- pancake vortices
(d) geometric effects --- Intermediate state
(e) surface superconductivity
Lecture 3: Models and theories of superconductivity
Thursday
Today

## Slide 2
Basic properties of SCs:
ZERO ELECTRICAL RESISTANCE – primary defining property; one of the hardest to explain
turns up
leveled off
gradually
abruptly
Good experimentalist – 1st observed phenomenon, then tried to the understand behavior.
Discovered:
were not
were
Defined critical temperature
Defined critical magnetic field
Defined critical current
Found that the impurity content was not important
(Anderson Theorem 1959)
Named it SUPRA-CONDUCTIVITY
IEEE Trans. Magnetic 23 (1987) -- 75th Anniversary
Physics Today 63, 9, 38 (2010) --- 100TH Anniversary
History of Discovery:
Studying normal metal conductance
* Nobel Prize 1913
First to liquefy helium
(phonons)
* Discovery: Heike Kamerlingh Onnes Leiden 1911 (April)

## Slide 3
Depends on purity and homogeneity
Broadened by magnetic fields and fluctuations
For comparison, “pure”
factor of lower
really small

1. How “zero” is the resistance?
Best results !
Advanced experiments to test
Apply magnetic field to induce a circulating current and monitor the decaying field in the loop for as long as you are willing to wait
Best result: Pb
τ
factor of lower!
It’s really zero!

SC ring
Two key questions:
2. How sharp is the transition? --- is it an abrupt or a gradual change
R

## Slide 4
Found this arXiv paper that purports to have proven that the resistance is exactly zero --- not sure, it does not seem to have ever been published

## Slide 5
2. CRITICAL TEMPERATURE/MAGNETIC FIELD/CURRENT
destroyed by current flow
[not strictly true --- as we will see, geometry & microscopic effects “pairbreaking” --- play a big role as well]
critical temperature
critical field
I
B
“Silsbee rule” - wire becomes normal when field at the surface reaches Hc
critical current
estroyed by temperature
destroyed by magnetic field

## Slide 6
constant
Maxwell’s equations :
ZERO FIELD-COOLED
For a perfect conductor, the state below depends on the history of the cooling
field excluded
FINITE
FIELD-COOLED
field trapped in
PERFECT DIAMAGNETISM ( )
Consider a perfect conductor
“Meissner effect”
Meissner
Ochsenfeld
Discovery : Walther Meissner and Robert Ochsenfeld 1933
This was a surprise – why?
Magnetic field excluded from
For a superconductor, the state below behaves as zero-field cooled always! inside (not only ρ

## Slide 7
Two possible descriptions to give these field behaviors:
(1) perfect diamagnetic material (local)
(2) screening supercurrents flow to screen fields (global)
Describe state as a PERFECT DIAMAGNET :
[cgs]
[MKS]
 this picture has some advantages for energy calculations
 this is the accurate physics description

## Slide 8
4. MAGNETIC FIELD PENETRATION
What we have discussed almost never occurs --- fields penetrate superconductors for many reasons:
(a) Penetration depth
  Effective diamagnetism caused by screening currents that flow over a finite thickness near edge
  “penetration depth”
  Fields penetrate into sample over this distance --- we will characterize this phenomenon in various electrodynamic and microscopic theoretical models

## Slide 9
(b) Type II superconductivity Shubnikov (experiments); Abrikosov (theory)
Most are Type II and allow flux penetration in discrete “vortices” of magnetic flux
Type I : elements 1% of all superconductors
Type II : alloys, compounds, thin films, dirty materials, disordered, unconventional, ..…
Key : surface energy positive (Type I) or negative (Type II) --- we will study the theory in depth
interface between N and S regions
*Important – allows at fields well above the 100 g/K region
(if NbTi were type I, Hc 1 KG instead of > 10 T)

## Slide 10
1. Two critical magnetic fields ( , )
field starts to penetrate
field fully penetrates (normal state)
Meissner
state
Abrikosov state
Mixed state
Vortex state
Phenomena:

## Slide 11
2. Hc2 field scale can be much larger
20
40
60
20
10

## Slide 12
Vortex state (H)
Maximize interface area subject to flux quantization constraint
Triangular lattice of vortices of flux
=
=

## Slide 13
See review by Blatter et al.
Irreversibility
Normal
Vortex
liquid
melting
Vortex
Lattice
(Vortex Glass)
Vortex
liquid
Meissner
HTSC are very anisotropic --- layered materials with weak interlayer coupling
This allows vortices to decouple between layers, giving rise to a complex vortex phase diagram
(c) Anisotropic materials
Pancake vortices in layered material
Abrikosov vortices in bulk material

## Slide 14
Screening of fields is affected by the geometry of the sample  demagnetizing effects
Inside:
Outside:
OUTSIDE:
UNIFORM
DIPOLE
RESULTANT
(d) Geometric effects --- the intermediate state
Consider a SC sphere:
B.C:
continuous
INSIDE:

## Slide 15
For ellipsoidal sample:
where e = eccentricity
In general, Define demagnetizing factor for each shape:
(inside)
(inside)
(outside)
Demagnetizing Factor D

## Slide 16
SOLUTION: system breaks up into N and S longitudinal
INTERMEDIATE STATE (between the Meissner and Normal states)
(like vortex state since flux penetrates but tries to minimize rather than maximize the amount of surface)
PARADOX: system cannot stay SC
system cannot go N (field penetrates so that H = Ha < Hc
edge cannot go N (still same problem)
Since Ht continuous, inside
Turn up applied field, >> before
Look at equator:
for D>0

## Slide 17
Field range:
Fields:
MEISSNER INTERMEDIATE NORMAL
Fraction of N material :
  Conserve flux through sample to determine :
In
In
(if more or less, interface would move as material goes )

## Slide 18
Derivation of expression :
Consider sample as having an “average” magnetization <M> less than perfect diamagnetism value:
Compare to <M> in laminar structure:
0

## Slide 19
Magnetic Properties (averaged properties)

## Slide 20
Intermediate state in Type II
Same effects below H – distorts magnetization

## Slide 21
Laminae Structures
COMPLEX structure and calculation
Ideal – depends on geometry, fields, boundary energy (N/S)
Real – also depends on surface condition and sample homogeneity
Best model: Landau Domain Theory
Add energies: condensation energy of
field energy of
spreading energy of field outside
wall energy
branching energy (domain broadening near the surface

## Slide 23
Surface
Vortex
Meissner
(e) Surface superconductivity
Nucleation offavored near the surface can exist at higher fields at surfaces
Physics: SC order parameter is suppressed at the surface (costing energy) but allowing field penetration (saving energy) --- we will see this trade-off in the Ginzburg-Landau model