## Slide 1
Lecture 4: Ginzburg-Landau Theory
Start discussion of how to understand the superconducting state
Present four phenomenological approaches:
Thermodynamics picture --- motivated by early experiments
Order parameter picture --- the Gorter-Casimir “two-fluid” model
Electrodynamics picture --- the London equations
Non-local electrodynamics model --- the Pippard extension to the London equations
Lecture 3: Models and theories of superconductivity
Next Tuesday
Today

## Slide 2
THEORIES OF SUPERCONDUCTIVITY
macroscopic problems (E&M)
spatial variations (intermediate/mixed state)
current applied
macroscopic quantum phenomena
1st principle calculations
Thermodynamic details
Excitations --- tunneling transport
electrodynamics
Phenomenological
Thermodynamics
Gorter-Casimir (two fluid)
London
Pippard
Ginzburg-Landau
Gorkov - Eliashberg (TDGL = Time-Dependent G-L)
Gorkov
Microscopic
BCS
+ Anderson
+ Bogoliubov
+ Midgal
Unconventional SC models
Which is right?
Which are useful?
For superconductor device physics and quantum information applications? need some of both

## Slide 3
Phenomena --- what were experiments saying?
SC was new (and unusual) – perfect conductivity and perfect diamagnetism
Sharp and reversible onset with temperature and magnetic field and current
THERMODYNAMICS
Compare “energy” of and states
internal energy
OK for isolated systems
Helmholtz free energy
constant
= Gibbs free energy
at the phase transition (i.e. at Tc or Hc)
New phase of matter with a phase transition
which thermodynamic energy is appropriate?
Must account for energy from field source since changes at transition (Meissner effect)
Compare and for same applied field and require that
OK for

## Slide 4
THERMODYNAMICS
1ST Law of Thermodynamics
2nd Law of Thermodynamics (quasistatic)
internal energy
heat input
work done BY system
constant
= applied magnetic field
= entropy

## Slide 5
(1) Normal state: independent of magnetic field for a non-magnetic material
(2) Phase transition:
(3) Superconducting state:
What do we know?
“Condensation energy” (stabilization energy)
Depends on T
perfect diamagnetism
SC is a lower energy phase that is weakened by applying magnetic field --- costs energy to expel the field
= in MKS units

## Slide 6
Independent of field
Entropy
for constant

## Slide 7
Normal state:
Comments: As , (for both states) as required by the 3rd law 
is an ordered state
Slope discontinuous at
(Sommerfeld constant)
Superconducting state:

## Slide 8
Latent heat (at transition)
In zero magnetic field, no latent heat because the transition occurs at , where
In finite magnetic field for T<Tc(H), transition by an applied field or an increase in T gives a finite latent heat
1st order in finite field
2nd order phase transition in zero field
(1st derivative of is discontinuous)
1st Order
2nd Order
(1st derivative of is continuous)

## Slide 9
Specific Heat
SC specific heat is higher
- cubic
+linear

## Slide 10
Normal state:
phonons
Preview of BCS:
electrons
Thermodynamic predictions:
Linear at low
Cubic at higher
Jump at
Jump precisely determined by
Exponential at low energy gap
Superconducting state:

## Slide 11
Two Fluid Model Gorter – Casimir (1934) (analogous to that in superfluid , but preceded it)
Thermodynamics + two fluids T-dependences of measurable quantities: and
Order parameter = fraction of SC electrons
NORMAL CARRIERS:
from
Then, phase equilibrium
(No information about )
1st guess:
2nd guess:
Then,
SC CARRIERS:
Minimize to get

## Slide 12
Choose
Calculate quantities:
Significance:
1st use of concept of an order parameter
Idea of a superfluid + normal excitations --- key concept of BCS and useful for transport and non-equilibrium effects
Focus on thermal properties --- gets right form for electrodynamics
so that
Interesting model but not very justifiable
density of superconducting electrons
Then,

## Slide 13
London Equations F. London, H. London (1935)
Focus on describing the electrodynamics Variation of with time, space (screening currents)
Forces:
=
1st London Equation
=
London Parameter
Fritz London
Heinz London
Return to the superconductor as a perfect conductor:

## Slide 14
2. Magnetic Fields:
1-D geometry
excluded from bulk (expected for perfect conductor)
Meissner effect
excluded
2nd London Equation
1st London Equation

## Slide 15
LONDON EQUATIONS
Can these be justified?
Start with the “canonical momentum”
Assume same at finite field.
We expect
in the ground state at zero field.
London equations

## Slide 16
Corrections:
superfluid part only
Normal fluid:
does not obey London
Comments:
(a) not gauge invariant
Valid only for London gauge:
(
at surface)
(b) “Rigidity” of wavefunction
 electrons not affected by a magnetic field
(c)
suggests “condensation” into
state
Bose pairing of electrons
Going back to the “two-fluid picture: London equation applies only to the superfluid part
superfluid density
includes chemical potential

## Slide 17
Applications
(1) Steady-state:
(2) Field expulsion:
Superconductor
50 nm
40 nm
85 nm
200 nm
NbTi 300 nm
65 nm
140 nm
YBCO (c) 700 nm
Al
Pb
Nb
PbBi
Nb3Sn
YBCO (a,b)
Temperature dependence:
Consistent w/ two-fluid model

## Slide 18
(3) Field applied to a finite thickness plate
Width =
B vs.
For different
B vs. x
For different

## Slide 19
(4) Current flow in a strip
(a) Current density (uniform):
But this will be modified to prevent field penetration into the sample
Self-fields from currents will be screened by SC

## Slide 20
(b) Self-consistent London solution
Solve for current flow
:
current conservation
For
uniform
For
current piles up on edge

## Slide 21
(5) Current flow at N-S interface
2-D problem inside
Boundary conditions:
Current constraint:

## Slide 22
Beyond London …..
limitations of the London equations:
(3) Predicts no dependence on impurities (contradicts experiment)
Sn + 3% In doubled
DIRTY
CLEAN
Determined from microwavwe wave absorbtion measurements of
in doped samples:
(1) Describe superfluid response – must put in normal response separately two-fluid model
(2) Applies to weak magnetic fields cannot handle vortices, intermediate state, inhomogeneous materials, …
(4) Local equations:

## Slide 23
Brian Pippard (Cambridge, 1953)
depends on a weighted-average of over a range coherence length
Pippard Non-local Modification to
LONDON
PIPPARD
How did he get this form?
CHAMBERS expression for non-local resistivity
(replacing )
Here, range of influence is due to memory over time between scattering events

## Slide 24
Range of non-locality for SC:
Pippard coherence length
DIRTY
CLEAN
Values of
DIRTY SC
~
CLEAN SC ()

## Slide 25
vs. LOCAL (London) vs. NON-LOCAL (Pippard)
Averages current from higher
effective increase in by
Non-locality:
>
<
~

## Slide 26
In CLEAN LIMIT, can be either London or Pippard limit:
LONDON
PIPPARD
In moderately DIRTY limit
In very DIRTY limit
Always in London (local) limit
Pippard expression:
DIRTY
CLEAN
PIPPARD SC
LONDON SC
Non-locality over the coherence length modifies the penetration depth depending on the impurity concentration: