## Slide 1
Lecture 5: Ginzburg-Landau theory --- surface energy and vortices
Lecture 4: Ginzburg-Landau Theory --- model and characteristic lengths
Next Tuesday
Today
Discussion the Ginzburg-Landau theory in three parts:
Presentation of the model and derivation of the penetration length and coherence length
Calculation of the surface energy and categorization of Type I and Type II superconductivity
Current-carrying states and phase coherence

## Slide 2
Brian Pippard (Cambridge, 1953)
depends on a weighted-average of over a range coherence length
Pippard Non-local Modification to
LONDON
PIPPARD
How did he get this form?
CHAMBERS expression for non-local resistivity
(replacing )
Here, range of influence is due to memory over time between scattering events

## Slide 3
Range of non-locality for SC:
Pippard coherence length
DIRTY
CLEAN
Values of
DIRTY SC
~
CLEAN SC ()

## Slide 4
LOCAL (London)
Averages in current from higher
effective increase in by ~
Non-locality:
>>
vs.
NON-LOCAL (Pippard)
Pippard penetration length:

## Slide 5
In CLEAN LIMIT
LONDON
PIPPARD
In moderately DIRTY limit
In very DIRTY limit
Always in London (local) limit
Pippard expression:
DIRTY
CLEAN
PIPPARD SC
LONDON SC
Non-locality over the coherence length modifies the penetration depth depending on the impurity concentration:
Pippard coherence length and non-locality was introduced to explain the impurity-dependence of the penetration depth
We will see a similar but different coherence length emerge from the Ginzburg-Landau theory

## Slide 6
GINZBURG – LANDAU THEORY (1950)
Phenomenological – allows for spatial variations of properties not
included in London equations (local electrodynamics)
Order parameter complex “wavefunction”
Superconducting electron density two-fluid model
Not widely outside Russia in the early days --- thought to be too phenomenological
1959 Gorkov (using thermal Green’s functions) showed that
GL BCS in limit of near , slowly varying fields and currents and
energy gap parameter (related to , gap in excitation spectrum)
BCS gap parameter which depends on qp’s
Now widely accepted and applicable to many problems
Vitaly Ginzburg
Lev Landau
Lev Gorkov
We will follow the presentation (by Ginzburg and Landau) --- not the microscopic derivation (by Gorkov)
--- until ---

## Slide 7
and free energy near phase transition in in zero field
Simplest possible form:
cannot expand in since G must be real
odd terms not allowed since G is analytic at
or else minimum at
Minimum at
Minimum at
NORMAL STATE
as before (G-C model)
GINZBURG – LANDAU MODEL
SUPERCONDUCTING STATE
“Mexican hat potential”
“Condensation energy”

## Slide 8
What about ?
NORMAL
TRANSITION
SC
What about ?
GL assumed constant
which is observed near
Finite fields allows currents, spatial variations:
MAGNETIC
With geometry effects (intermediate state):
”
”
If field penetrates, energy required to expel field is smaller

## Slide 9
ELECTRONIC
kinetic energy
for
gradients in (interface N-S)
kinetic energy of pairs (supercurrent)
All quantities obtained from 2 experiments vs. and vs. all thermodynamics, electrodynamics, complex cases where fields and currents vary (e.g. intermediate state)
GL only strictly valid at but extensions to lower are useful and often give useful results

## Slide 10
Ginzburg-Landau Theory
Free energy:
CONDENSATION
ENERGY
KINETIC ENERGY
MAGNETIC FIELD
EXPULSION
(1)
(2)
wrt and
order parameter
magnetic fields
No fields
Fields minimize total of sample
GL differential equations:

## Slide 11
Boundary conditions:
(sufficient to give no current flow)
(necessary for current-carrying states)
finite for normal metals,
for magnetic materials (no SC)
G-L
deGennes
for insulator
finite
(normal metal)
(magnetic material)
(insulator)

## Slide 12
ISOLATED SAMPLE – no transport currents
real (choose proper gauge)
Notes:
(1) LOCAL theory
(2) EXPANSION in is strictly only valid near but works more widely
(3) SPATIAL theory – allows varying fields and currents
(4) PHENOMENOLOGICAL - can be determined from measurements ofand (via )
, uniform
using
in anticipation of BCS

## Slide 13
Length Scales
Variation of penetration depth
(regain London for constant)
(# pairs)
Variation coherence length
Assume no fields
Assume no currents real
Define
using
since
Define natural length scale:
using
coherence length

## Slide 14
Relation to Pippard coherence length:
No reason why they should be related --- not based on the same physics
independent of
Diverges at
Connection via BCS theory:
clean limit
dirty limit
Note: dependence on also different

## Slide 15
Physical meaning:
range of non-local averaging
range of order parameter variations
Let (perturbation to the bulk order parameter)
Sets range for decay of order parameter (cubic term vital)
Scale over which can change with out large cost in free energy
Pippard :
Ginzburg-Landau :

## Slide 16
Define parameter:
dependence:
constant
dependence:
constant
BCS:
clean limit
dirty limit
ratio of 2 lengths
Type II
Type I
CLEAN
DIRTY
Material | Tc(K) | (nm) | 0(nm) | 
Al | 1.2 | 50 | 1600 | 0.03
Sn | 3.4 | 50 | 230 | 0.22
Pb | 7.0 | 40 | 83 | 0.48
Nb | 9.2 | 85 | 38 | 2.24
PbBi | 8.3 | 200 | 20 | 10
NbTi | 9.5 | 300 | 4 | 75
Nb3Sn | 18 | 65 | 3 | 22
YBCO (a,b) | 95 | 140 | 1.5 | ~100
YBCO (c) | 95 | 700 | 0.3 | ~1000

## Slide 17
GL equations couple and so expect to depend on field penetration
Assume  small neglect terms in and assume to get an estimate for
GL2:
GL1:
THICK SAMPLE
Variation of Order Parameter near a surface
(Type I)
B.C. at surface

## Slide 18
Double exponential in and
Suppression of order parameter in field
INCREASING
Full self-consistent solution shows deviation of x) from exponential