## Slide 1
Lecture 6: Ginzburg-Landau Theory --- current-carrying states and phase coherence
Lecture 5: Ginzburg-Landau theory --- surface energy and vortices
Thursday
Today
Discussion the Ginzburg-Landau theory in three parts:
Presentation of the model and derivation of the penetration length and coherence length
Calculation of the surface energy and categorization of Type I and Type II superconductivity
Current-carrying states and phase coherence

## Slide 2
Ginzburg-Landau Theory (summary)
G-L free energy:
CONDENSATION
ENERGY
KINETIC ENERGY
MAGNETIC FIELD
EXPULSION
Minimize wrt
(1)
(2)
Order parameter
Superelectron density
ISOLATED SAMPLE – no transport currents, real
coherence length
penetration length
G-L parameter
Interplay of the order parameter and magnetic fields
phase

## Slide 3
GL equations couple and so expect to depend on field penetration
Assume  small neglect terms in and assume to get an estimate for
GL2:
GL1:
THICK SAMPLE
Variation of Order Parameter near a surface
(Type I)
B.C. at surface

## Slide 4
Double exponential in and
Suppression of order parameter in field
INCREASING
Full self-consistent solution shows deviation of x) from exponential as well
Expect (suppressed by field)
GL2:
increased by the suppression of
MEDIUM SAMPLE
What happens in a thinner sample? a slab or a thin film
field can vary
uniform order parameter
Calculated in Lecture 3 using the London equations

## Slide 5
suppresses grows and drops
At some point transition
This defines a critical field H (parallel)
at the phase transition
(thin films),
For (thick films), partially suppressed at the transition
For
at the S  N transition
GL1:
2nd
order
1st
order

## Slide 6
THIN FILMS d << and d <<
when
Why? because the field does not have to fully exclude the field from bulk to maintain SC
Relevant for Type II
p = 0
From before:

## Slide 7
Surface Energy
Calculate contributions to Gibbs free energy at interface
field repulsion energy
condensation energy
Allow field penetration lowers SC energy
Lose SC region raises SC energy
, since H = Hc at the phase boundary
Bulk:
Surface: (integrate over surface region)

## Slide 8
N-S boundaries cost energy
Resists formation of vortices
N-S boundaries lower the system energy
Encourages formation of vortices
g = energy per length
Ginzburg – London treatment
Subtract from expression
using and
1st GL equation:
Multiply by and integrate

## Slide 9
field
penetration
order parameter
variation
Solve , from GL calculate ,
B
B
Self-consistently, variation of
I
x
B
Limits:
① small
Assume no field penetration:
, for

## Slide 10
② large
Better, consider variation which cannot be neglected due to terms. Find:
③ (crossover region)
But phase coherence plays a key role in the nature of vortex state
Assume
I
x
B
This will determine whether a material is
Type I
Type II

## Slide 11
Type II Superconductivity
VORTEX STATE
(2) Fluxoid quantization smallest flux unit
B
VORTEX
NORMAL
MEISSNER
H
Vortex density:
Triangle lattice more stable (barely)
SURFACE
MEISSNER
NORMAL
VORTEX
nucleation of SC at surface
nucleation of SC in bulk
flux entry into SC
field penetrates in discrete vortices
(1) negative surface energy maximize N-S interface area

## Slide 12
VORTEX STRUCTURE
Abrikosov vortex
core
Near core, dominated by
Far away, ’ dominated by
Quantization  at all r
B
I I I I
r
I I
r
We will show next time that the quantity that is quantized is the “fluxoid” (not the magnetic flux):
’= + =
B varies over
(2) varies over
(3) B flattens off near core because
--- defines “core” of the vortex

## Slide 13
Nucleation of SC in the bulk
When does SC start as is lowered?
Neglect cubic term – valid for
which will occur at high fields as onsets
since corrections are of order this decouples the two GL equations into one for
Assume
(gauge choice)
Use linearized GL equation:

## Slide 14
Harmonic oscillator Schrödinger equation with potential:
“spring constant”
“equilibrium position”
“oscillation frequency”
Solutions are quantized state called Landau levels:
Choose greatest for and :
(first solution at highest)
“upper critical field”
Wavefunction:
nucleation of at
using
and

## Slide 15
For
at fields above due to flux penetration
For
supercooling before before onsets
Has been observed --- can be used to measure but is usually destroyed by surface roughness Actually, will only supercool to (where surface onsets)
Type II SC
1st order transition
2nd order transition

## Slide 16
Surface
This neglects fall off of at surface (over)
Energy lower at surface forms at higher value of
Supports layer of of with width
Can get ’s with 1st order but no supercooling

## Slide 17
Vortex Nucleation: when do vortices enter as raises?
Define critical field
At
Let line energy of vortex/length
Tradeoff vortex energy vs. field energy (to allow to penetrate)
1 vortex
0 vortices
“lower critical field”

## Slide 18
? Must solve to get vortex slope:
Calculate line energy (field energy +
Guess:
field
energy
condensation
energy
Solutions use full
zero – order Hankel function
(long range)
(short range)

## Slide 19
does not diverge in core – flattens off as near center
Put back in:
areas equal